## Slide 1: Cracks and its Repair
Dr. Safeer Abbas
Assistant Professor
Civil Engineering Department
UET Lahore, Pakistan
Notes: My name is Safeer Abbas. I did my BSc Civil Engineering from UET Lahore, Pakistan. Then, I started my Master degree at UBC Vancouver Canada in September 2008. I joined Dr. Nehdi’s research group as a PhD candidate in September 2010.
And today I am going to defend my PhD thesis on the “Structural and Durability Properties of Precast Segmental Tunnel Linings.”
As the name indicate, my research focused on two aspects of PCTL. First the structural performance mainly related to flexural and thrust load resistance and secondly, durability performance mainly related to chloride induced corrosion.

## Slide 2: Differential Settlement
Inadequate Design
a) Inadequate concrete thickness
b) Inadequate steel
c) Inadequate non uniform soil support
d) Incorrect geometry
e) Incorrect use of materials

## Slide 3: Cracks Readings
Orientation, location, Length, Width, Depth, Shape, Frequency, age

## Slide 4: Combined Shear and Axial Stress

## Slide 5: Example: Wall Supporting Slab

## Slide 6: Cavitation
Cavitation causes erosion of concrete due to collapse of vapour bubbles formed by pressure changes in high velocity water flow.
Vapour bubbles form and flow downstream. When they enter a zone of high pressure, they collapse with great impact. The energy released called cavitation, causes damage to concrete.
Cavitation forms near curves and offsets or at the center of vortices.
Can be reduced by producing smooth surfaces and avoiding protruding obstructions to flow.

## Slide 7: Abrasion
Abrasion is wearing away of the surface of concrete by rubbing and friction. Factors affecting abrasion resistance are:
Compressive strength.
Aggregate properties.
Finishing methods.
Use of toppings
Curing

## Slide 8: Crack Evaluation, Causes and Scope
User needs:
Useful life
Urgency
Cost
Performance requirements
Aesthetics

## Slide 9: Repair Analysis and Strategy
Structural needs
Effect of repair on & compatibility with existing structure
Constructability
Environment
Safety Repair Strategy
What is expected of surface repair?
Surface deterioration diverse in nature
Goal: Protection, appearance, load carrying
Function of repair determines properties of repair material to be specified

## Slide 10: Surface Preparation and Bond
Clean sound substrate
Rough profile - - - mechanical anchorage
Open pore structure
Repair material absorption into
substrate
Intimate contact

## Slide 11: Proper Surface Preparation: Bond Mechanism

## Slide 12: Reinforcing Steel Preparation
Abrasive blast
Water blast
Combination blasting
Degree of cleanliness required
Bar coating

## Slide 13: Bonding Agent Problems

## Slide 14: Intimate Contact
Form & pump, vibration, hand pressure, apply spray

## Slide 15: Quality Assurance: Achieving Bond
Testing Bond strength
Laboratory testing (ASTM C-881, 1042)
Slant shear
Result depend upon: substrate strength, surface preparation
Direct shear (Shear bond)

## Slide 16: Quality Assurance
Uni-axial tensile strength
Visual evaluation

## Slide 17: Bond Failure Causes

## Slide 18: Bond Failure
Incomplete surface preparation
Bruising
Micro-fracture
Important Points:

## Slide 19: Repair Materials
Considerations: Strength, durability, chemical resistant, compatibility with substrate
Requirements:

## Slide 20: Strength

## Slide 21: Durability

## Slide 22: Chemical Resistance

## Slide 23: Repair Materials
Latex modified concrete
Polymer concrete
Rapid setting concrete
Shotcreting
Sealers:
Prevent water from entering concrete surface
Permit water vapour to escape

## Slide 24: Sealer Problems/Concerns
Lack of penetration
Poor surface penetration
Excessive moisture
Rapid evaporation due to wind and temperature condition

## Slide 25: Should a Crack be Repaired
Considerations
Structural versus non-structural
Crack width and length
Crack location within a member
Environmental exposure conditions
Type of member
Appearance

## Slide 26: When Should a Crack be Repaired?
At what point should the width of a crack be a concern?
If the only criteria is load transfer across the crack (0.64 mm --- 0.025 in)
Research has shown that load transfer due to aggregate interlock is almost fully effective across the cracks of 0.025 in. or less. Load transfer across cracks of 0.035 in. is good, but not fully effective.
However, durability of concrete is important as the load transfer characteristics. Durability is enhanced by preventing moisture reaching the embedded rebars.

## Slide 27: Crack Repair Using Epoxy Injection
Characteristics of Epoxies
Excellent adhesive properties
Versatile
Chemical resistant
Rapid curing
Resistant moisture
To restore tensile strength to a cracked concrete members e.g. Beams, slab etc

## Slide 28: Crack Repair using Epoxy Injection
Typical Installation Procedure
Prepare surface, seal crack and install injection ports, inject resin, cure, grind off seal and ports

## Slide 29: Common Installation Problems
Improper resin
Improper mixing
Inadequate surface sealing
Improper pressure
Improper port spacing
Improper sequence of
pumping
Excessive crack width

## Slide 30: Trial Repair Method: Gravity Feed

## Slide 31: Trial Repair Method: Flood Coating

## Slide 32: Trial Repair Method: Epoxy Injection